# YD 180 AL

## Model:

## QZYL/180, EI/AIWA/180

## Description:

## YD 180 AL, is polyesterimide enamelled aluminium wire belonging in H (180°C) thermal class, able to be manufactured in the diameter range of 0.20 – 3.66 mm. Provides advantage due to the low density of aluminum in cases where weight is more important than volume.

## Available:

### Providing thermal resistance up to 180 °C, YD 180 AL offers ease of winding due to the flexible enamel layer coated on soft conductor.

## Fields of Use:

- Contactor

- Magnetic coils

- Relays

- Transformer

- Small motors

- Ballast

## Advantage:

- All products parameters are recorded with quality control system at every stage of production process and following by barcode system until delivery.

- Our products receive approval with production parameters of quality control system according to standards of GB/T23312.7 2009, IEC60317-25, NEMA 35.

| Thermal Class (°C) | Class H, 180 °C |
| --- | --- |
| Insulation ¦ Base Coat | Polyester-imide |
| Insulation ¦ Top Coat | - |
| Insulation ¦ Bong Coat | - |
| Production Range (MM) (MM) | 0.20 - 3.66 mm |
| Certification I.E.C | IEC 60317 - 15 |
| UL File No. |  |
| Class Temperature (°C) | 180 °C |
| Heat Shock (°C) | ≥ 200 °C |
| Cut Through Temperature (°C) | ≥ 320 °C |
| Solderability (°C) | Non solderability |
| Bonding Temperature (°C) | Not Applicable |
| Re-softening Temperature (°C) | Not Applicable |
| Normal Solvent Resistance | 3H-4H |
| Resistance to humidity | Excellent |
| Resistance to Impregnants | Yes |
| Resistance to Refrigerants | Yes |
| Distinct Features | Generator, Motors, Transformers |